| Parameter | Omnibus 4 | XR5TM |  | Units |  |
| --- | --- | --- | --- | --- | --- |
|  | typical value’s | typical value’s |  |  |  |
| Signal to Noise ratio (108μlx) | 24 | 28 |  |  |  |
| Limiting resolution | 64 | 70 |  | lp/mm |  |
| MTF (contrast) at: |  |  |  |  | *1 |
| 2,5 lp/mm | 90 | 93 |  | % |  |
| 7,5 lp/mm | 80 | 82 |  | % |  |
| 15 lp/mm | 61 | 67 |  | % |  |
| 25 lp/mm | 38 | 46 |  | % |  |
| 32 lp/mm |  | 35 |  | % |  |
| Luminance gain at 2.10-5 lx | 50.000/π | 50.000/π |  | cd/m2/lx |  |
| E.B.I. (dark noise) | 0.25 | 0.25 |  | μlx |  |
| Wavelength band | 550 – 900 | 350 – 900 |  | nm |  |
| Life time | 10000 | >15000 |  | hours | *2 |
| Over illumination protection | vulnerable | protected |  |  |  |
| Luminance dynamic Range | 1.0E-06/ 1E-01 | 1.0E-06/5.0E+04 |  | lux |  |
| Shock resistance | 75 | 500 |  | g’s |  |
| Halo size | ± 2.0 | ± 0.4 |  | mm | *3 |
| Gate voltage | 800 | Automatic |  | V |  |
| Formats | 18 | 18 /retrofit |  | mm |  |
| Export restrictions | US-export restricted | no US restrictions |  |  | *4 |

remarks:

- The better contrast in the mid line-pair range has more contribution to a good overall performance than the absolute limiting resolution

- XD-4TM photocathodes are much less vulnerable to ion feedback than the GaAs photocathodes.

- The halo’s in XD-4TM tubes are not only smaller but also less intense.

- Because DEP does not rely on US ITAR components no DSP-83 form is required, which makes much faster delivery times possible.